# KRONOTEX EXQUISIT PLUS

| Test | Characteristics | Test method |
| --- | --- | --- |
| Formaldehyde emission | < 0.05 ppm | EN 717-1 |
| Surface stain resistance | Grade 5, no visible changes to surface | EN 438-2, 15 |
| Lightfastness | ≥ Level 6 Blue Wool Scale ≥ Level 4 Grey Scale | EN ISO 105-B02 EN 20 105-A02 |
| Resistance to cigarette embers | Grade 4, no visible changes to surface | EN 438-2, 18 |
| Fire resistance | Ignites with difficulty, at least Cfl-s1 | EN 13501-1 |
| Height difference between connected elements | Average: ≤ 0.10 mm max: ≤ 0.15 mm | EN 13329 |
| Edge straightness (bend) | ≤ 0.3 mm/m | EN 13329 |
| Openings between connected elements | Average: ≤ 0.15 mm max: ≤ 0.20 mm | EN 13329 |
| Static indentation | < 0.01 mm - no visible changes, Impression in test with straight steel cylinder of 11,3 mm diameter | EN 433 |

| Strength | Thermal conductivity (W / (m × K)) | Overall heat transfer coefficient Thermal resistance ((m² × K) / W) |
| --- | --- | --- |
| 8 | 0.13 | 0.06 |

# KRONOTEX EXQUISIT PLUS

## EXQUISIT PLUS – TIMELESS COMPANION

Perfection in panel form: With the EXQUISIT PLUS collection, you can easily create a feel-good atmosphere. The extra-wide panels in various natural wood looks invite you to create an ambience of elegance and generosity. Feel the combination of warmth and nature – noble and high-quality, furnished with embossed grain and a matt shimmer. The precisely milled V-groove completes the convincing appearance, as you would expect from a plank floor. That is the perfection you dream of.

- Decors

- Information

- Specifications

- Product Range

- Installation instructions

### Abrasion Class 
Commercial 32 AC 4

### Decor Properties

Wide

These panels are especially wide.

Structure

These panels have a special surface structure.

Clic System

A 5G snap-together system makes the flooring even easier to install.

V4 - all the way round

These panels are equipped with a 45° bevelled edge all around. When joined together, a V-groove is created, which conveys a natural solid wood plank character.

Optimised Joints

Thicker laminate flooring panels also have thicker CLIC snap-together joints.

### Certificates

### General approval for use in construction by Deutsches Institut für Bautechnik (German Institute for Civil Engineering)