# KRONOTEX GLAMOUR ﻿

| Test | Characteristics | Test method |
| --- | --- | --- |
| Resistance to abrasion | AC4 | EN 13329 |
| Impact resistance | IC 1 | EN 13329:2006, Appendix F |
| Resistance to stains | 5 (groups 1 und 2) 4 (group 3) | EN 438-2 |
| Behaviour with cigarette burns | Grade 3 | EN 438-2 |
| Behaviour during simulation of movement of the leg of a piece of furniture | no visible change when performing the test with leg type 0 | EN 424 |
| Thickness swell | ≤ 18.0 % | EN 13329:2006, Appendix G |
| Property | Requirements | Test method |
| Humidity content at the time of dispatch from the factory | The elements must have a humidity content of 4% to 10 %. The humidity content of a delivery must be even at Hmax – Hmin < 3 % | EN 322 |
| Appearance, surface defects | Minor surface defects as defined in EN 438-5 are permissible. | EN 438-2 |
| Behaviour when exposed to scratching | The elements must exhibit, as a minimum, level 3 resistance to scratching in accordance with EN 438-2. | EN 438-2 |

| Strength | Thermal conductivity (W / (m × K)) | Overall heat transfer coefficient Thermal resistance ((m² × K) / W) |
| --- | --- | --- |
| 8 | 0.13 | 0.06 |

### Abrasion Class 
AC 4

### Decor Properties

Wide

These panels are especially wide.

Long

These panels are especially long.

High gloss surface

High gloss surface

Clic System

A 5G snap-together system makes the flooring even easier to install.

V4 - all the way round

These panels are equipped with a 45° bevelled edge all around. When joined together, a V-groove is created, which conveys a natural solid wood plank character.

Fast Installment

Fast installment thanks to an easy-to-use angle-angle locking system for the long and short sides of the boards.

Optimised Joints

Thicker laminate flooring panels also have thicker CLIC snap-together joints.

### Certificates