KRONOTEX MAMMUT PLUS
	Test 
	Characteristics 
	Test method 

	Formaldehyde emission 
	< 0.05 ppm 
	EN 717-1 

	Surface stain resistance 
	Grade 5, no visible changes to surface 
	EN 438-2, 15 

	Lightfastness 
	≥ Level 6 Blue Wool Scale 
≥ Level 4 Grey Scale 
	EN ISO 105-B02 
EN 20 105-A02 

	Resistance to cigarette embers 
	Grade 4, no visible changes to surface 
	EN 438-2, 18 

	Fire resistance 
	Ignites with difficulty, at least Cfl-s1 
	EN 13501-1 

	Height difference between connected elements 
	Average: ≤ 0.10 mm 
max: ≤ 0.15 mm 
	EN 13329 

	Edge straightness (bend) 
	≤ 0.3 mm/m 
	EN 13329 

	Openings between connected elements 
	Average: ≤ 0.15 mm 
max: ≤ 0.20 mm 
	EN 13329 

	Static indentation 
	< 0.01 mm - no visible changes, Impression in test with straight steel cylinder of 11,3 mm diameter 
	EN 433 



	Strength 
	Thermal conductivity (W / (m × K)) 
	Overall heat transfer coefficient Thermal 
resistance ((m² × K) / W) 

	10 
	0.14 
	0.075 
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Abrasion Class 
Commercial 33 AC 5 
Decor Properties 
[image: Long]
Long 
These panels are especially long. 
[image: Wide]
Wide 
These panels are especially wide. 
[image: Structure]
Structure 
These panels have a special surface structure. 
[image: Clic System]
Clic System 
A 5G snap-together system makes the flooring even easier to install. 
[image: V4 - all the way round]
V4 - all the way round 
These panels are equipped with a 45° bevelled edge all around. When joined together, a V-groove is created, which conveys a natural solid wood plank character. 
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Antistatic 
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